## Supplemental Information

## Aged osteoporotic bone marrow stromal cells demonstrate defective recruitment, mechanosensitivity, and matrix deposition.

Michele A. Corrigan1,2, Siobhan Coyle3,4, Kian F. Eichholz1,2, Mathieu Riffault1,2, Brian Lenehan3,4, David A. Hoey1,2,5*

1Trinity Centre for Biomedical Engineering, Trinity Biomedical Sciences Institute, Trinity College, Dublin, D02 R590, Ireland

2Dept. of Mechanical and Manufacturing Engineering, School of Engineering, Trinity College Dublin, Dublin 2, D02 DK07, Ireland

3Department of Trauma and Orthopaedics, University Hospital Limerick, Limerick, Ireland

4Graduate Entry Medical School, University of Limerick, Limerick, Ireland

5Advanced Materials and Bioengineering Research Centre, Trinity College Dublin & RCSI, Dublin 2, D02 VN51, Ireland

Short Title: Defective hMSCs in setting of osteoporosis

*Corresponding Author

Prof. David A. Hoey

Dept. Mechanical and Manufacturing Engineering

Trinity Centre for Biomedical Engineering

Trinity College Dublin

Dublin, Ireland

Tel: 00353 1 896 1359

E-mail: dahoey@tcd.ie

Keywords: Bone; Mesenchymal stem cells; Osteoporosis; Mineralisation; Oscillatory fluid shear

Supplementary Information

Supplementary Methods:

Quantification of coverage of culture surface by stained monolayer

The surface area covered by positively stained monolayer was quantified by limiting the threshold of 8-bit images between 135 and 255 in Image J, so as to highlight stain free regions. Areas below threshold were selected and the sum of the areas of these regions was calculated. The below threshold area was subtracted from the total area of each image to calculate the area covered by stained matrix, the data was converted to percentage for presentation in Supplementary Figure 2. For each healthy and osteoporotic sample of MSCs % coverage was measured for one representative image.

Supplementary Table 1: The sequences of the primers used to quantify gene expression in MSCs

| Gene | Forward Primer | Reverse Primer |
| --- | --- | --- |
| 18S | ATCGGGGATTGCAATTATTC | CTCACTAAACCATCCAATCG |
| COX2 | AAGCAGGCTAATACTGATAGG | TGTTGAAAAGTAGTTCTGGG |
| OPN | GACCAAGGAAAACTCACTAC | CTGTTTAACTGGTATGGCAC |
| RUNX2 | GCAGTATTTACAACAGAGGG | TCCCAAAAGAAGTTTTGCTG |
| TRPV4 | GATCTTTCAGCACATCATCC | GGTCATAAAGCGAGGAATAC |

Supplementary Figures:

Supplementary Figure 1: Representative images of Alcian blue stained pellet cultures of each sample following 21 days culture in chondrogenic differentiation medium, 4x scale bar =500µm, inset is at 10x, scale bar =100µm, n=2-4.

Supplemental Figure 2: % of the surface area covered by Picrosirius (top) and Alizarin (bottom) stained monolayer in healthy and osteoporotic MSCs in growth or osteogenic medium, n=3, Mean +/-SEM.

Supplemental Figure 3: A Quantification of DNA content following  21 days in growth medium or adipogenic, Mean±SEM, n=4, two-way ANOVA with Bonferroni post test  B, C Representative images of Oil Red O stained monolayers of B Healthy and C Osteoporotic samples following 21 days culture in growth or adipogenic differentiation medium, 2x scale bar=1000µm, inset at 10x scale bar=200µm, n=3. D-G Quantification of adipogenic matrix in each sample D, E concentration of lipid extracted from D individual samples and E samples pooled based on health (µg/ml), Mean±SEM, two-way ANOVA with Bonferroni post test, ***p<0.001, differentiation medium effects the samples differently p<0.001 (interaction effect), n=4. F, G  Oil Red O concentration normalized to DNA content (ng/ml) for F each sample and G pooled concentration of collagen in healthy and osteoporotic samples, N=3.